Reconnaissance Survey (G4) for Glauconite and associated mineralization In Dhamni-Piparwasi Simliya area, Sheopur district, Madhya Pradesh

Litholog: DPS/BH/01

| Agency | Maheshwari Mining Pvt Ltd |
| --- | --- |
| Date of Commence | 04-05-2025 |
| Date of Closing | 08-05-2025 |
| Easting | 734452.9 |
| Northing | 2864576 |
| RL | 297.7743 |
| Lattitude | 25:52:50.94191 |
| Longitude | 77:20:23.81120 |
| BH NO | DPS/BH-01 |
| Azimuth | Vertical |
| Inclination | Vertical |

| Lithology From_Depth (m) | Lithology To_Depth (m) | Lithology contact angle | Lithology True Width (m) | Lithology Name | Lithology Description | Structures | Stratigraphic Unit |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 4.5 | NA | 4.5 | Loose Material | Green to Brown color soil, mainly composed of clay and silt particles loose soil material also have broken pieces of sandstone of 1 to 2 inches and cores of boulders of up to inches. |  | Govindgarh Formation Rewa Group Vindhyan Supergroup |
| 4.5 | 8.5 | 90⁰ | 4 | Shale with sandstone intercalations | Greenish-grey weathered shale, fine-grained and thinly bedded, with sub-centimeter partings. Some core segments are completely weathered, resulting in poor or no recovery. The shale is composed primarily of clay minerals and quartz. Intercalated within the shale are medium-grained, light grey sandstone layers with sub rounded and moderately sorted grains. Glauconite mineral grains are visible within the sandstone bands, indicating marine depositional influence. | Laminations |  |
| 8.5 | 10.5 | 90⁰ | 2 | Sandstone with shale intercalation | Grey sandstone, fine- to medium-grained, occurring in core segments of 3 to 5 inches thickness. Grains are sub-rounded and moderately sorted. The sandstone is primarily composed of quartz, with subordinate feldspar and rare glauconite grains. Occasional lithic fragments are also observed. A distinct glauconitic band (~5 inches thick) is present at approximately 9 meters depth. Some portions of the core show signs of weathering and are discontinuous. Minor intercalations of shale occur between sandstone beds, indicating periodic shifts in depositional energy and environment. | Bedding of thin to medium thickness |  |
| 10.5 | 16.50 | 90⁰ | 6 | Shale | Black color, evenly laminated, fresh shale with partings at less than one to eight inches, some discontinuous light green color lamination also presents with clay minerals, shale is calcareous, showing mind effervescences and 10 to 19 percent CaO present in geochemical analysis, secondary fillings are common in partings, mostly concordant but some are at angle with lamination plane, some secondary fillings are composed of sulfides while others are of Calcite. | Laminations |  |
| 16.5 | 24.8 | 90⁰ | 8.3 | Sandstone | Highly compact, fresh, fine grained, Dull white color, sorted, rounded and medium to thickly bedded, mainly composed of quartz but disseminated altered light green color grains are also present. Color changes from light grey to dark grey at the both ends of this unit adjacent to shale unit | Thin to Medium bedding |  |
| 24.8 | 31 | 90⁰ | 6.2 | Shale and sandstone intercalations | Dark grey shale with laminations is intercalated with grey color sandstone, sandstone is fine grained composed of quartz and some grains of glauconite and feldspar. | Thin bedding and laminations |  |
| 31 | 34 | 90⁰ | 2 | Shale | Black color, evenly laminated, fresh shale with partings at less than one to eight inches, secondary fillings are common in partings, mostly concordant but some are at angle with lamination plane. |  |  |